## Slide 1
Project Title: | Effect of Dopant on Acetone Gas Sensing Properties of Sn2O Nanostructures
Synopsis: | According to the World Health Organization (WHO), diabetes is among the top 10 causes of global death, killed 1.6 million people in 2016. At present, the detection methods used for these diseases are invasive and expensive. It has been reported that the exhaled breath of patients suffering from diabetes have a higher concentration of acetone gas. The acetone concentration in the breath from a healthy human body is lower than 0.9 ppm and it is higher than 1.8 ppm for a diabetic patient. So, it is of great significance to develop a highly sensitive and selective acetone gas sensor for non-invasive diagnosis of diabetes. N-type metal oxide semiconductors are suitable in sensing reducing gases. Among the large number of n-type metal oxides, SnO2 is one of the most concerned gas sensing materials. However, gas sensors based on metal oxide semiconductors always operate at high temperature, which had high energy consumption, thus limiting the application of these sensing materials. The incorporation of different materials such as carbon based materials and conducting polymers with metal oxide semiconductors have attracted much attention for the construction of high-performance breath gas sensors due to the synergistic effect of two individual materials. In this project the effect of dopant of different kind of materials such as carbon based materials and conducting polymers on acetone gas sensing properties of SnO2 nanostructures will be investigated. The morphological and structural properties of nanocomposite will be analysed by different characterization techniques such as FESEM, EDX, XRD, RAMAN and FTIR spectra.
Objectives: | To synthesis nanocomposites based on SnO2 nanostructures as a sensing material using hydrothermal method To fabricate acetone gas sensor based on as-prepared nanocomposites To investigate the effect of dopant of different kind of materials such as carbon based materials and conducting polymers on acetone gas sensing properties of SnO2 nanostructures
Equipment required: | Gas sensing setup, FESEM, EDX, XRD, RAMAN and FTIR
Software required: | Microsoft excel, Origin
Supervisor (Department): | Prof. Dr. A. S. M. A. Haseeb (Mechanical)
Program: | Master of Engineering (Materials/Mechanical)
Duration: | Maximum 2 consecutive semesters

## Slide 2
Project Title: | Mechanical performance of advanced multicomponent solder alloy for electronic packages
Synopsis: | An innovative solder alloy was created recently by adding different elements Sn/Ag/Bi/Sb/Cu/Ni-X in certain percentage. This novel solder material lacks scientific data and requires a lot of characterization work to justify the reliability of it. As compared to the conventional Sn/Ag/Cu solders, the life time in thermal cycling test was longer in industrial report. However, tensile test of dog bone shape sample of this sample under thermal aging condition according to JEDEC standard was not studied. In this research, the newly created solder will be aged under different temperature and duration, then tensile tests under different strain rates will be conducted and the fracture surfaces would be observed and analysed. Besides, microstructures of the solder cross section with different test condition will be observed and hardness will be checked under micro indentation. In the end, characterization and reliability of this solder will be summarized.
Objectives: | To test the mechanical properties of a new solder alloy with thermal aging. To observe the microstructure changing of the solder cross section with different test conditions. To create a numerical model to predict the relationship between aging and mechanical properties of this new solder alloy.
Equipment required: | Temperature chamber, Tensile test machine, FeSEM, EDX, TEM, XRD, Grinding and polishing machine, Micro indentation
Software required: | ANSYS Workbench
Supervisor (Department): | Prof. A. S. M. A. Haseeb (Mechanical)
Program: | Master of Material Engineering
Duration: | Maximum 2 consecutive semesters

## Slide 3
Project Title: | Effects of temperature in electrochemical migration of tin
Synopsis: | As the pitch size in electronic packages decreases due to miniaturization, problems related to electrochemical migration (ECM) become a serious reliability concern. ECM is an electrochemical reaction that occurs in presence of electrolyte and bias voltage, causing metallic components to dissolve at the anode and redeposit at the cathode in the form of dendrites leading to short circuit failure. Electronic devices are subjected to a wide range of temperatures during service. This work investigates ECM process of tin at different temperatures (27°C – 90°C). The effects of temperature on the mean time to failure and the mechanism of ECM will be investigated. The model which describes the relation between the time to failure (TTF) of ECM and the environmental temperature will be established. The characterizations of the products of ECM include FESEM/ EDX.
Objectives: | To study the effects of varying temperature on ECM of tin To establish model which describes the relation between the time to failure (TTF) of ECM and the environmental temperature To identify the products of ECM of tin at different temperatures
Equipment required: | Semiconductor Characterization System(SCS); FESEM/ EDX
Software required: | Kiethley Interactive Test Environment (KITE); ANSYS; IC Measure
Supervisor (Department): | Prof. Dr. A. S. M. A. Haseeb (Mechanical)
Program: | Master of Engineering (Mechanical/Materials)
Duration: | Maximum 2 consecutive semesters

## Slide 4
Project Title: | In-situ study of electrochemical migration of tin in presence of contaminants
Synopsis: | As the pitch size in electronic packages decreases due to miniaturization, problems related to electrochemical migration (ECM) become a serious reliability concern. ECM is an electrochemical reaction that occurs in presence of electrolyte and bias voltage, causing metallic components to dissolve at the anode and redeposit at the cathode in the form of dendrites leading to short circuit failure. Contaminants originating from manufacturing process steps, flux residue and environment can accelerate the process. This work investigates ECM process of tin (Sn) in the presence of different contaminants, for example sulphates and glutaric acid by water drop test (WDT). The effects of different contaminants on the mean time to failure (MTTF) and the mechanism of ECM will be investigated.
Objectives: | To study the effect of various contaminants on the ECM MTTF of Sn. To investigate the ECM mechanism in the presence of contaminants. To improve ECM reliability of Sn in electronic interconnections.
Equipment required: | Semiconductor Characterization System, Field Emission Scanning Electron Microscope (FESEM), Energy-dispersive X-ray spectroscopy (EDX)
Software required: | Keithley Interactive Test Environment (KITE) software
Supervisor (Department): | Prof. Dr. A. S. M. A. Haseeb (Mechanical)
Program: | Master of Materials Engineering
Duration: | Maximum 2 consecutive semesters

## Slide 5
Project Title: | Polyurethane foam scaffold mechanical characterization for biomedical application
Synopsis: | Polyurethanes are versatile biomaterials explored for various biomedical applications due to their superior biocompatibility and biodegradability properties. Polyurethane mechanical properties are adjustable depending upon the composition and specific ratios of the soft and the hard segments used. Various biomedical applications require specific mechanical properties of the underlying polyurethane scaffolds. Thus, apart from spectroscopic characterization including UV-VIS, FTIR, NMR and MS required for structural elucidation of the polyurethane scaffolds, there is a strong need for the mechanical testing of the polyurethane scaffolds including hardness, Young’s modulus, tensile strength and elongation at rupture of polyurethane scaffolds under different temperature, humidity and strain rate conditions to optimize their mechanical properties for the desired biomedical application.
Objectives: | To investigate polyurethane scaffold mechanical properties including hardness, Young’s modulus, tensile strength and elongation at rupture. To establish relation between polyurethane structure and mechanical properties under different temperature, humidity and strain rate condition. To determine and optimize mechanical properties of the polyurethane scaffolds for the desired biomedical application.
Equipment required: | Universal testing machine/ Nano hardness tester
Software required: | OriginPro
Supervisor (Department): | Prof. A. S. M. A. Haseeb
Program: | Master of mechanical/materials Engineering
Duration: | Maximum 2 consecutive semesters